## Slide 1: Nonlinear Analysis Based on Unstable Modes in Amorphous Solids
Kota Noto, Kuniyasu Saitoh(A),
Harukuni Ikeda, Hisao Hayakawa
YITP, Kyoto Sangyo Univ.(A)
July 9th, 2025
Mini-workshop on "Jamming, rheology and granular matter“
@ YITP K202

## Slide 2: Outline
Introduction
Derivation of Unstable Modes with Wavenumber
Weakly Nonlinear Analysis for Unstable Modes

## Slide 3: Granular material
Granular materials governed by repulsive interactions in amorphous solids
Macroscopic objects at T = 0, negligible thermal fluctuations
Energy dissipation plays a major role
Powder
Sand
Ball

## Slide 4: Hessian Matrix
Eigenvalue analysis of 2N degree
: corresponding to curvature of PEL
:Potential energy
particle configuration of i-th particle (-cordinate)
: eigenvector field
PEL in a 2N-dimention
We can get other property
(Shear modules ,,, )
Notes: 不均一な系のため、解析に粒子配置を用いる。

## Slide 5: Unstable Particle Configuration
Repeatedly performing eigenvalue analysis for different particle configurations is necessary.
C. E. Maloney and A. Lemaître PRE (2006)
E. Lerner, Phys. Rev. E 93, 053004, (2016)
F. Ebrahem et al., Phys. Rev. E 102, 033006 (2020).
Motivation
・Focus on configurations with negative eigenvalues.
・Analyzed configurations that become unstable with a single perturbation from the initial condition.
D. Ishima et al., PRE 2023
Anharmonic
Harmonic

## Slide 6: Nonlinear Analysis of Amorphous Solids
NQE(Nonlinear quasilocalized excitations)
Case for Positive Eigenvalues
→ Apply Negative mode
Luka Gartner and Edan Lerner, Phys. Rev. E 93, 011001(2016)
Geert Kapteijns et al., Phys. Rev. E 101, 032130 (2020)
NPM(Nonlinear plastic modes),

## Slide 7: Hessian matrix including wavenumber
Dispersion relation
S. Schoenholz et al. Soft Matter, 9, 11000 (2013).
Hessian matrix
Hessian matrix including wavenumber
Get negative eigenvalue!
Notes: 今までの解析は、k = 0の正の固有値のみを用いて行われてきた。
システムに負の固有モードが存在する場合、
変形を加えた際の応答を
理論解析およびシュミレーションを用いて確かめる。

## Slide 8: How introduce wavenumber
:Particle index
:Cell index
: Center of -th cell
= Re{}
: Spring constant
In the case of 1d3atoms chain、
Equation of motion
Put plane wave anzats
Notes: 周期境界ではない。
異なるセルにおける同一粒子に対して、異なる変位を許す。
a crystal-like tiling structure where each unit cell contains an amorphous region”
“a tile-like structure that resembles a crystal but has an amorphous configuration within each unit cell”

## Slide 9: Linear response
For any initial condition,
only the negative modes become dominant
Solution obtained by applying initial conditions
Positive: Oscillation
Negative: Divergence
Plane wave can be rewritten for arbitrary displacement as:
: Displacement of
the reference cell
Notes: An arbitrary displacement can be expanded in terms of eigenvectors

## Slide 10: Use Edge Mode
Case: -> Wavelength =
Deformation of X mode
infinite system
2cell system
The outer boundary is periodic.

## Slide 11: Deformation corresponding to wavenumber
Y : Stable Case
X : Unstable Case
Case: -> Wavelength =
①lowest eigenvector
:lowest eigenvectors of edge mode
Isotropic compression at pressure P
Notes: 固有値が波数に対応しているため、変形も波数に対応する必要がある。
そのため、波数に対応した変形を考える。
“Since the wavelength at the edge wavenumber is 2L, the deformation can be captured using a system with two unit cells. Therefore, we analyze this two-cell configuration below.”

## Slide 12: Setting of sumilation
2D
1:1.4 , 1:1, frictionless
Harmonic Potential:
P =
Pressure controlled initialization using pressure studs
Number of Particles in a cell: N = 8 ~ 2048
Fast Inertial Relaxation Engine (FIRE)
: step function
P>0
P<0

## Slide 13: Lowest eigenvector
Stable case
Unstable case
Returns to the original state after deformation
Amplifies the deformation further
deformation
response
deformation
Response
→Unstable modes can be captured！
×50
Notes: 拡大率： Magnification
Scale Factor

## Slide 14: Deformation corresponding to wavenumber
Case: -> Wavelength =
①lowest eigenvector
② sinusoidal transverse wave
③ square transverse wave
Three type of deformation
:lowest eigenvectors
Isotropic compression at pressure P
Notes: 固有値が波数に対応しているため、変形も波数に対応する必要がある。
そのため、波数に対応した変形を考える。
“Since the wavelength at the edge wavenumber is 2L, the deformation can be captured using a system with two unit cells. Therefore, we analyze this two-cell configuration below.”

## Slide 15: Response of various perturbations
Sinusoidal wave
Square wave
The responses are independent of the initial perturbations.
Lowest eigenvector

## Slide 16: Outline
Introduction
Derivation of Unstable Modes with Wavenumber
Weakly Nonlinear Analysis for Unstable Modes

## Slide 17: Weakly nonlinear analysis
・ negative eigenvalue system
Overdamped equation
Weakly nonlinear analysis
Negative: Divergence
Oscillation term aaaa
Notes: We expand the potential to higher-order terms to capture nonlinear effects.
expand the potential to higher-order terms

## Slide 18: Nonlinear equation
Put ansatz
evaluated at the saddle point
We get bellow equation
Notes: take a contraction of the tensor

## Slide 19: Time Evolution
Then, we obtain
・Amplitude
・Potential

## Slide 20: Comparison with simulations
• Quantitatively different, qualitatively consistent
η Dependence
Notes: “This is the plot when η is varied. The potential change does not perfectly match, but the response agrees quantitatively when the parameter is varied.”

## Slide 21: Comparison with simulations
-
P =

## Slide 22: Summary
We investigated the response of a system with negative eigenmodes by applying external perturbations.
Regardless of the type of perturbation, the negative eigenmode dominates, leading to the same response.
Weakly nonlinear analysis supports the relationship between the energy decrease and the corresponding eigenvalue.